## Slide 1: NANOSCALE SILICON CMOS RESPONSE TO THz RADIATION FOR TESTING VLSI
Michael Shur1,2 and John Suarez3
Presented at NAST
Essex, Vermont
May 8, 2018
1 Electronics of the Future, Inc.,
Vienna, VA 22181, USA
and
2 Rensselaer Polytechnic Institute
Troy, NY 12180, USA
3 US. Army CERDEC,
Aberdeen Proving Ground, Aberdeen, MD 21005, USA

## Slide 2: Outline
Motivation
THz plasmonics for testing Si MOSFETs and VLSI
Defect THz signatures
Future work
Conclusions

## Slide 3: Number of transistors on chip

## Slide 4: VLSI layers: 14 layers
Cross-section SEM of three 150-nm 1.5V fully depleted SOI CMOS tiers showing oxide bonds and 3D via interconnects between circuit levels, including 3 transistor levels and 11 metal interconnect levels.
Image from https://www.ll.mit.edu/mission/electronics/qiin/cmos-technology/3d-integration-of-CMOS.html

## Slide 5: Complexity

## Slide 6: Moore’s Law versus Inverse Moore’s Law
Inverse
Moore’s Law

## Slide 7: Previous approach: I7 fragment transmission image: 5 x 5 mm2, f=288 GHz (mm resolution)
mm
mm

## Slide 8: New approach: use voltages induced by THz beam at the MMIC or VLSI pins

## Slide 9: THz Radiation impinging on a FET couples via contacts and interconnects and induces a DC voltage
Drain
Source
2D Channel:
Gate
L
THz
ΔU~P
9
ΔUgs
ΔUgd
Your text here
Notes: 9

## Slide 10: These voltages are induced because of plasma waves launched and rectified by FET nonlinearities
High frequency, high mobility detector
Lower frequency, lower mobility detector where Lo is the characteristic length of the decay of the plasma wave excited at source side
A. Gutin, V. Kachorovskii, A. Muraviev, and M. Shur, "Plasmonic terahertz detector response at high intensities," Journal of Applied Physics, vol. 112, pp. 014508-014508-5, 2012.

## Slide 11: THz SPICE Model
A. Gutin, T. Ytterdal, V. Kachorovskii, A. Muraviev, and M. Shur, THz SPICE for Modeling Detectors and Non-quadratic Response at Large Input Signal, IEEE Sensors Journal, Vol. 13, Issue: 1, pp. 52-62 (2013)

## Slide 12: Experimental setup for nanoscale resolution

## Slide 13: Measured and simulated 40 nm FINFET response
From W. Stillman, C. Donais, S. Rumyantsev, M. Shur, D. Veksler, C. Hobbs, C. Smith, G. Bersuker, W. Taylor and R. Jammy, Silicon FIN FETs as detectors of terahertz and sub-terahertz radiation, International Journal of High Speed Electronics and Systems, vol. 20, No. 1, pp. 27-42 March (2011)
20 fin nFET open drain response, normalized to response maxima, across several incident frequencies. Wf = 40 nm; Lg = 100 nm. Dashed line represents modeled response with f = 0.2 THz.
Above and below
threshold model

## Slide 14: 1 to 77 GHz Medium Power Amplifier TGA4706-FC. 14 dBm output power at 77 GHz
PHEMT Product Qualification Report TGC4703-FC, TGC4704-FC, TGA4705-FC, TGA4706-FC, http://documents.tips/documents/triquint-psg-low.html

## Slide 15: Transfer current voltage characteristics at dc terminals for separate transistors in virgin TGA4706-FC MMIC
Transistor 1 damaged
Virgin
S. Rumyantsev, A. Muraviev, S. Rudin, G. Rupper, M. Reed, J. Suarez and M. Shur, Terahertz Beam Testing of Millimeter Wave Monolithic Integrated Circuits, IEEE Sensors Journal, IEEE Sensors J., Vol. 17, NO. 17, Sep. 17, 5487. (2017)

## Slide 16: Response to sub terahertz radiation at dc terminals
Transistor 1 damaged
Virgin
S. Rumyantsev, A. Muraviev, S. Rudin, G. Rupper, M. Reed, J. Suarez and M. Shur, Terahertz Beam Testing of Millimeter Wave Monolithic Integrated Circuits, IEEE Sensors Journal, IEEE Sensors J., Vol. 17, NO. 17, Sep. 17, 5487. (2017)

## Slide 17: Frequency shift of CMOS ring oscillator vs. oscillator base frequency and supply voltage
From M. Shur. THz Sensing Technology, Special issue of the International Journal of High-Speed Electronics, and System sand A. hardcover book, Vol. 24, Nos. 1 & 2 (2015), DOI: 10.1142/S0129156415500020
Incident 1.5 mW , 0.2 THz beam focused to 1.5 mm spot diameter

## Slide 18: Polarization, temperature, bias, intensities dependencies, and space scans of THz response form parts of the fault signatures
Space scan
Polarization
Temperature
Bias

## Slide 19: Intensity dependence
Gutin A., Kachorovskii V., Muraviev A., and Shur M., "Plasmonic terahertz detector response at high intensities," Journal of Applied Physics, 112, 014508-5 ( 2012)

## Slide 20: Future work
Signature identification at the model validation stage
Signature identification during reverse engineering
Reliability/lifetime prediction
Hardware (cyber) security – faked versus genuine parts
Cyber defense applications

## Slide 21: CONCLUSIONS
THz radiation effectively couples to FET (including Si CMOS)
At low THz intensities, the response is proportional to the THz intensity
THz response detects difference in
  Gate leakage
  Mobility
  Threshold voltage
THz response detects faults under bias
Nanometer scale resolution
Scanning a VLSI chip allows for generating a large number of test vectors